TECHNICAL SHEET  - POLYETHYLENE PACKAGING

# PRODUCT:	 Rubbish bags in various dimensions, thicknesses and colours

| Rubbish Bags with star sealing, simple sealing ( in rolls) naturel and coloured ( printing) Minimum thickness :17 microns Maximum thickness: 60 microns | minim value width =200mm maxim value width =840 mm minim value length=100mm maxim value length = 2000mm |
| --- | --- |

OBTAINING

Material:

The packaging are produced from the recipes with minimum 80% PCR plastic recyclate  , the dimensions according to the customer's requirements.

###### TECHNICAL QUALITY CONDITIONS

| Nominal thickness | Thickness tolerance |
| --- | --- |
| Up to 15 µ | ± 15% |
| 15 - 25 µ | ± 10 % |
| Over 25 µ | ± 7 % |

The length of bag/sack : ± 5 % tolerance allowed

The width of bag/ sack : ± 5 % tolerance allowed

Execution: Polyethylene foil packaging is made by cutting and welding the foil.

Appearance: The bags from polyethylene must be smooth, without breaks, holes, stains, foreign objects or other deficincies that would lower the resistance. There are allowed longitudinal stripes or light folded from winding of foil, but they must not affect the quality (shape) of final product.

The walls of packaging should be easily to open, slide. The polyethylene foil packaging is natural in color, unprinted, according to the beneficiary's request. The welding of the foil must be continuous, the packaging does not stick together.

Colour. The colour of foil will be natural/different colours.

Rules for quality control

Checking the quality of polyethylene foil packaging is done on batches consisting of the same type of packaging, the same method of execution and the same size. When checked, the product must comply with the customer's requirements and the required technical quality conditions.

Control methods

Checking the dimensions.

Checking the length and width is done with ordinary measuring instruments.

The thickness is checked with the micrometer.

The checking of appearance and color is done visually by comparison with standard samples.

Packaging, labeling, storage, transport

The polyethylene foil packaging are placed in cardboard boxes .

A label with the following specifications shall be applied to each box:

- the name of products ;

- dimensions of product ;

- quantity / box.

Or any other information required by the customer.

Polyethylene foil packaging must be stored in a clean, dry room, away from any source of heat or direct sunlight.

Transport of polyethylene foil packaging must be done with covered and clean means of transport.

Documents

Each order/batch of delivery will be accompanied by a quality certificate, packing list, invoice and other legal documents.

Influence on the environment

Polyethylene bags are part of recyclable packaging. Packaging waste can be recovered by grinding, regranulation, with the condition that the packaging from which the waste is coming, has not been in contact with chemicals or toxic materials. The mill or re-granules thus obtained may be reintroduced in manufacturing products that do not come in direct contact with food (e.g. construction foils).

Other specifications

October 2023

# Text boxes

The product beeing from plastics product category is in fuel  Class A, respectively „Usual flammable materials: wood, paper, clothing, plastics".

Calorific values of polyethylene is 43 MJ / kg.